Source model

Transport type- neutron and photon transports

Averaged source energy:

neutron energy 2.3 MeV

photon energy 0.66 MeV

Detector model:

Detector crystal: Cd (Z=48) 90% and Zn (Z=30) 10%

*In current version of the MCNP code, cross sections of elements like Ge, Te etc are missing!

Geometry of the model

neutron/gamma-ray source, CdZn detector, sample holders, radiation protection and moderator

84cm

27 cm

Parafin protection

Thickness 4 cm

Ø=0.3 cm

4 cm

CdZn detector

Sample

n-Source

Lead holder

parafin

moderator

7.5 cm

Lead protection

Thickness 5 cm

Samples:

Simulation

1.82 MeV

2.24

.3.56

5.16

5.92

6.42

4.95

2.05

4.42

1.82 MeV

2.24

.3.56

5.16

5.92

6.42

4.95

2.05

4.42

Table 1. PGNAA simulations of Dolerite stone samples

| Chemical element | Major gamma-ray | D.Pch2 | D.Sky1 |
| --- | --- | --- | --- |
|  | MeV | Peak area | Peak area |
| Ca | 1.94 | 15.3 | 15.9 |
|  | 4.42 | 6.06 | 5.69 |
|  | 6.42 | 2.2 | 2.29 |
| Si | 1.16 | 50 | 50 |
|  | 2.09 | poor | poor |
|  | 3.54 | 6.5 | 6.8 |
|  | 3.66 | poor | 4.6 |
|  | 4.93 | 6.5 | 6.6 |
|  | 6.38 | 1.7 | 1.93 |
| K | 0.77 | poor | poor |
| Al | 4.13 | poor | 3.7 |
|  | 4.69 | poor | 3 |
|  | 4.91 | poor | poor |
|  | 5.13 | poor | poor |
| Fe | 7.65 | poor | poor |

Table 2. PGNAA simulations of Granite stone samples

| Chemical element | Major gamma-ray | G.Pch1 | G.Pch2 |
| --- | --- | --- | --- |
|  | MeV | Peak area | Peak area |
| Ca | 1.94 | 11.8 | 13.8 |
|  | 4.42 | 4.13 | 3.3 |
|  | 6.42 | 1.65 | poor |
| Si | 1.16 | 47 | 48.3 |
|  | 2.09 | poor | poor |
|  | 3.54 | 7.3 | 8.26 |
|  | 3.66 | poor | poor |
|  | 4.93 | 7.5 | 7.34 |
|  | 6.38 | 2 | 3 |
| K | 0.77 | poor | poor |
| Al | 4.13 | poor | poor |
|  | 4.69 | poor | poor |
|  | 4.91 | poor | poor |
|  | 5.13 | poor | poor |
| Fe | 7.65 | poor | poor |

Gamma-ray emission simulation

Monte Carlo simulations

Monte Carlo simulations using MCNP-5 code and the ENDF/B-VI cross section data set were performed in order to evaluate PGNAA analysis for two types of stone sample. The model included the source, collimator, gamma ray detector, shielding, moderator and the sample. The developed model enabled prediction of voluminous source gamma ray detector efficiency for the characteristic prompt-gamma rays of the elements of interest.